## Slide 1: Na Diffusion in NaSiCON
Zeyu Deng (Jerry)

## Slide 2: Natrium Superionic CONductor (NaSiCON)
Na1+xZr2SixP3-xO12 (0 ≤ x ≤ 3)
High conductivity: 15 mS/cm at x = 2 ~ 2.4 studied by Hong and Goodenough in 1976 for the rhombohedral phase
2 Na(1) sites, 6 Na(2) sites and 6 Si/P sites
Phase behavior knowledge and kinetics are limited because of the complexity of the crystal structure
Challenges: Disordering, large structure and flat energy landscapes.
Deng, Z.; Sai Gautam, G.; Kolli, S. K.; Chotard, J.-N.; Cheetham, A. K.; Masquelier, C.; Canepa, P. Phase Behavior in Rhombohedral NaSiCON Electrolytes and Electrodes. Chem. Mater. 2020, acs.chemmater.0c02695.
Goodenough, J. B.; Hong, H. Y.-P.; Kafalas, J. A. Fast Na+-Ion Transport in Skeleton Structures. Mat. Res. Bul. 1976, 11 (2), 203–220.

## Slide 3
Model Construction
build_model.py
Model Fitting
fit_model.py
Kinetic Monte Carlo
run_kmc.py
Results Analysis
Diffusivity
Conductivity
kmc.py
gather_mc_data.py
Calculate the Kinetics of Na in NaSiCON from First Principle
DFT-NEB Simulations
Why Kinetic Monte Carlo (KMC)?
Speed and accuracy
Direct calculation using structure-property relationship
Properties at finite temperature and different composition
For complex and disordered structure
Hamiltonian
NEB Barriers
Basis (Clusters)
Trajectories
Canonical Monte Carlo Simulations
Initial Structures
NEB = nudged elastic band

## Slide 4: Model Construction
4 Å

## Slide 5: Model Construction
Diffusion is always between a Na(1) site and a Na(2) site
Diffusion barrier is a local property and can be approximated by the kinetically resolved barrier EKRA
Vorbit is the kinetic effective cluster interactions (KECI), V0 is the empty cluster and ɸorbit is the cluster function for each orbit
A series of EKRA were computed for different local environments (occupations) and then Vorbit and V0 can be fitted from equation
A. Van Der Ven, Z. Deng, S. Banerjee and S. P. Ong, Chem. Rev., 2020, 120, 6977–7019.

## Slide 6: Model Construction
Cluster
cluster type
structure
Orbit
clusters
multiplicity
Event
na1_index
na2_index
sym
max_length
min_length
bond_distances
sorted_sublattice_index
occ_sublat
ekra
probability
corr
get_cluster_function()
get_cluster_function()
LocalClusterExpansion
clusters
orbits
sublattice_indices
cluster_constructor()
orbit_constructor()
A cluster (𝛼) is a collection of sites (i) (not atom)
An orbit (o) is a collection of symmetrically equivalent clusters
A diffusion event is a diffusion between 2 Na sites with information of the orbit and cluster around it
Occupation (σ) is ±1 for each sites depends on its occupation, e.g. Na or Vacancy (Chebyshev basis)
Cluster function (ɸ) is the product of all occupations in this cluster
Correlation (ɸo) is a vector of summation of all symmetrically grouped cluster functions for each orbit (ɸ𝛼)

## Slide 7: Model Construction
Type | Site Index | max_length | min_length | Multiplicity
point | (0,) | 0 | 0 | 6
point | (6,) | 0 | 0 | 6
pair | (0, 1) | 4.727 | 4.727 | 6
pair | (0, 3) | 5.103 | 5.103 | 6
pair | (0, 6) | 3.71 | 3.71 | 6
pair | (0, 7) | 3.056 | 3.056 | 6
pair | (0, 8) | 3.162 | 3.162 | 6
pair | (0, 9) | 6.492 | 6.492 | 6
pair | (0, 11) | 6.196 | 6.196 | 6
pair | (6, 7) | 4.922 | 4.922 | 6
pair | (6, 9) | 5.629 | 5.629 | 6
triplet | (0, 1, 6) | 4.727 | 3.162 | 6
13 Orbits generated using cutoffs: pair = 6.5 Å, triplet = 4.8 Å, quadruplet = 0.0 Å
Na, Si = -1
Va, P = +1

## Slide 8: Model Construction
0_0Si3P_0Si3P.cif [1, 1, 1, 1, 1, 1, 1, 1, 1, 1, 1, 1]
2_0Si3P_0Si3P.cif [1, -1, -1, -1, -1, 1, 1, 1, 1, 1, 1, 1]
2_0Si3P_1Si2P.cif [1, -1, -1, -1, -1, 1, 1, 1, 1, -1, 1, 1]
2_0Si3P_2Si1P.cif [1, -1, -1, -1, -1, 1, 1, 1, 1, -1, 1, -1]
2_0Si3P_3Si0P.cif [1, -1, -1, -1, -1, 1, 1, 1, 1, -1, -1, -1]
2_0Si3P_3Si0P_CB.cif [1, 1, -1, -1, -1, 1, 1, 1, 1, -1, -1, -1]
2_1Si2P_1Si2P.cif [1, -1, -1, -1, -1, 1, 1, 1, -1, -1, 1, 1]
2_1Si2P_2Si1P.cif [1, -1, -1, -1, -1, 1, 1, 1, -1, -1, 1, -1]
2_1Si2P_2Si1P_CB.cif [1, 1, -1, -1, -1, 1, 1, 1, -1, -1, 1, -1]
2_1Si2P_3Si0P.cif [1, -1, -1, -1, -1, 1, 1, 1, -1, -1, -1, -1]
2_2Si1P_2Si1P.cif [1, -1, -1, -1, -1, 1, -1, 1, -1, -1, 1, -1]
2_2Si1P_3Si0P.cif [1, -1, -1, -1, -1, 1, -1, 1, -1, -1, -1, -1]
2_3Si0P_3Si0P.cif [1, -1, -1, -1, -1, 1, -1, -1, -1, -1, -1, -1]
3_3Si0P_3Si0P.cif [1, -1, -1, -1, -1, -1, -1, -1, -1, -1, -1, -1]
Occupation (σi) used for DFT NEB calculations:
[[ 6. 6. 6. 6. 6. 6. 6. 6. 6. 6. 6. 6. 6.]
[-2. 6. -2. -2. -2. -2. -2. -2. -2. 6. 6. -2. -2.]
[-2. 4. -2. -2. 0. 0. -4. -4. 0. 2. 2. 0. -4.]
[-2. 2. -2. -2. -2. 2. -2. -2. -2. 2. -2. 2. -2.]
[-2. 0. -2. -2. 0. 0. 0. 0. 0. 2. -2. 0. 0.]
[ 0. 0. -2. -2. 2. -2. 2. -2. -2. 2. -2. 0. 4.]
[-2. 2. -2. -2. 2. 2. -6. -6. 2. -2. -2. 2. -6.]
[-2. 0. -2. -2. 0. 4. -4. -4. 0. -2. -2. 4. -4.]
[ 0. 0. -2. -2. 2. 2. -2. -6. 2. -2. -2. 4. 0.]
[-2. -2. -2. -2. 2. 2. -2. -2. 2. 2. -2. 2. -2.]
[-2. -2. -2. -2. -2. 6. -2. -2. -2. -2. -2. 6. -2.]
[-2. -4. -2. -2. 0. 4. 0. 0. 0. 2. 2. 4. 0.]
[-2. -6. -2. -2. 2. 2. 2. 2. 2. 6. 6. 2. 2.]
[-4. -6. 2. 2. 4. 4. 4. 4. 4. 6. 6. -2. -2.]]
Correlation (ɸorbit) computed from occupation
ɸ[orbit0]
ɸ[orbit12]
σ[site0]
σ[site11]
nsample
nsample
morbit
isite

## Slide 9: DFT-NEB calculations
https://www.scm.com/doc/AMS/Tasks/NEB.html
NEB = nudged elastic band

## Slide 10: DFT-NEB calculations
x ~ 0
x ~ 3
x = 2 for different local Si/P environment
Na1+xZr2SixP3-xO12 (0 ≤ x ≤ 3)
Na(1)
Na(2)
Na(1)
Na(2)
Na(2)
Na(1)
Na(2)
Na(1)
try 2x2x1 cell

## Slide 11: Model Fitting
Lasso Regression (L1 regularization):
minimizing the cost function
w is the weight for each orbit, is an energy penalty added to regularize our model and ɑ is a parameter chosen to minimize the CV error.
Quality of the fitting: Cross validation (CV) error and root mean square (RMS) error
V1
V2
Linear regression minimum
Lasso regression minimum
Prediction Error
Model Complexity
under fit
over fit

## Slide 12: Model Fitting
Predicted EKRA vs DFT calculated EKRA
Type | Site Index
point | (0,)
point | (6,)
pair | (0, 1)
pair | (0, 3)
pair | (0, 6)
pair | (0, 7)
pair | (0, 8)
pair | (0, 9)
pair | (0, 11)
pair | (6, 7)
pair | (6, 9)
triplet | (0, 1, 6)
Lasso Results:
KECI =
[ 0. 5.8 -4.47 -0. -12.94 -0. -0. -2.73 -5.09 0.
0. 3.85 0. ]
There are 6 Non Zero KECI
Empty Cluster =
314.08731330138085
index NEB LCE NEB-LCE
[[ 1. 236.15 220.66 15.49]
[ 2. 445.75 391.63 54.12]
[ 3. 352.85 357.13 -4.28]
[ 4. 397.35 383.84 13.51]
[ 5. 313.08 342.76 -29.69]
[ 6. 268.3 323.03 -54.73]
[ 7. 320.62 312.78 7.83]
[ 8. 307. 322.64 -15.64]
[ 9. 186.35 239.62 -53.27]
[ 10. 394.09 318.75 75.34]
[ 11. 301.15 288.53 12.62]
[ 12. 346.65 376.06 -29.41]
[ 13. 315.9 315.25 0.65]
[ 14. 311.95 254.43 57.52]
[ 15. 153.15 179.62 -26.47]]
CV = 75.12 meV
RMSE = 37.51 meV

## Slide 13: All barriers from local cluster expansion
charge neutral structure only
0_0Si3P_0Si3P.cif [1, 1, 1, 1, 1, 1, 1, 1, 1, 1, 1, 1]

## Slide 14: Kinetic Monte Carlo
Event update
…
Rejection free KMC
are random numbers
is related to vibrational entropy
Event propose
Generate Events
Load Occupations
Events Initialization
Compute the corr, ekra and probability for all events
Run KMC
only need one time for all calculations
from canonical monte carlo simulation
Initialization
Propose Event
Update Event
Summary
occupation, correlation, EKRA, probability and time
Na diffusion
Update Tracker
displacement for each Na
Na location, hop_counter
events and tracker
calculate DJ, D*, f and conductivity
Run KMC
repeat n_kmc steps
Event
na1_index
na2_index
sorted_sublattice_index
occ_sublat
ekra
probability
corr
Tracker
na_locations
hop_counter
displacements
calc_D_J()
calc_D_tracer()
calc_correlation()
calc_conductivity()
Single KMC run
repeat n input structures

## Slide 15: Kinetic Monte Carlo
Na | Na_locations | Displacement r(t)-r(0) | hop_counter
0 | 4 | [-10,3,12] | 138
1 | 20 | [4,2,1] | 152
2 | 5 |  | 146
… | … | … | …
n_Na | 3 | [23,21,52] | 165
Initialization
Propose Event
Update Event
Summary
occupation, correlation, EKRA, probability and time
Na diffusion
Update Tracker
displacement for each Na
Na location, hop_counter
events and tracker
calculate DJ, D*, f and conductivity
Run KMC
repeat n_kmc steps
Tracker stores information for each Na
Tracker
  na_locations
  hop_counter
  displacements
  calc_D_J()
  calc_D_tracer()
  calc_correlation()
  calc_conductivity()
Tracker has functions to analyze trajectory
n = <hop_counter>
a = 3.478 Å

## Slide 16: Resource Estimation
Total number of KMC runs for at a single temperature:
25 pass * 100 structures * 13 compositions * 8*8*8*8 Na/Va sites = 133.12*106 KMC steps
Time costs to complete these KMC runs at a single temperature using 8 nodes on NSCC
133.12*106 KMC steps / 3800 steps per min per core / 60 mins per hr / 24 cores/8 nodes = 3.04 hrs

## Slide 17: Clarification of some Terminologies
Concentration
Thermodynamic factor
Jump Diffusion Coefficient DJ
Diffusion Coefficient D
Tracer Diffusion Coefficient D*
Haven’s ratio
Correlation factor
Conductivity
Thermodynamic factor = 1 for non interacting intercalation (dilute), deviate 1 for ordering and high x
HR = 1 for no correlation between diffusing atoms, for electrolyte (constant x and nondilute), HR is less than 1
f = 1 for no correlation between successive hops of the same atom
comp(a) is the parametric composition
D_J is usually greater than D* because there are interactions among Na